 PIECE OF PERMANENT MAGNET 
	Specification Material 
	IEC Code 
	Magnetic Properties 

	Alnico 5 
	R1-1-1 
	Residual Induction 

Br [mT] 

1180 
	Coercive Force 

Hc [kA/m] 

48 
	Intrinsic Coercive Force 

Hci [kA/m] 

49 


 Requirements 
- Delivery not magnetized 

	Table Code 
	Type 
	Diameter D [mm] 
	Width W [mm] 
	Height H [mm] 
	Hole d [mm] 
	Volume min. [mm³] 
	Weight [kg] 

	76478023 
	EKAA 1 
	40 
	35 
	19,7 
	10 
	21920 
	0,17±0,005 

	Order related information 
	Use 

	MDF code: 5AC 

Order unit: pcs 
	- Permanent magnet of exciter 



[image: image1.png]H$0,2

#D+0,5

~—MAGNETOINTI
SUUNTA
DIRECTION OF

MAGNET IC





Needed for one 

EKAA 1 


8 pcs

_1367649587

